# PART 1 - GENERAL

1.1	DESCRIPTION

.1	Provide synthetic slate – Class A Tile Roofing System as specified and indicated on drawings; after the complete removal and proper disposal of the existing slate roof system while maintaining the building in a watertight condition.  Provide owner unit pricing for wood deck replacement.  Remove and reinstall the existing snow guard system.  The contractor will be responsible for repairing and/or replacing any parts to insure aesthetics and function.

.2	Provide Majestic Slate – Class A Tile Roof System in strict accordance with specifications and drawings approved by roofing product manufacturer.

.3	Related Work

.1	Metal flashing work is specified elsewhere in Division 7.

.2	Provide all associated roof products by the manufacturer; EcoStar attic guard ridge ventilation product must be used on those projects that will be using a ridge ventilation system.

1.2	QUALITY ASSURANCE

.1	Contractor shall be an authorized applicator approved by roofing

product manufacturer.

.2	There shall be no deviation made from this specification without

written approval from the owner and the roofing product manufacturer prior to the start of the roofing project.

.3	Warranty – Upon completion of the installation, an inspection must

be conducted by a technical representative of the roofing product manufacturer to ascertain that the roofing system has been installed according to most current published specifications and details.  This inspection is not intended to be a final inspection, but for the benefit of manufacturer; 10 year warranty is required.

.4	It is the roofing contractor’s responsibility to adhere to all applicable

building codes (local and national) and to have or acquire the appropriate licenses and permits, including open flame permit.

1.3	SUBMITTALS

.1	Submit manufacturer's product data, installation instructions and

general recommendations for each specified sheet metal and fabricated product.

.2	Submit shop drawings of fabricated sheet metal assemblies indicating

shapes, materials, thicknesses, fastening methods, and relation of adjacent construction.  Field verify existing dimensions and conditions prior to commencement of shop drawings to the greatest extent possible.

1.4	PRODUCT DELIVERY, STORAGE AND HANDLING

.1	Deliver materials in original unopened packages.

.2	Packages shall be labeled with manufacturer’s name, brand name,

installation instructions and identification of various items.

.3	All tile materials must be stored between 45ºF and 80ºF.  If exposed

to lower temperatures, restore to 45ºF minimum temperature before using.

.4	Store all materials in a dry protected area.  Damaged materials must

not be used.  Installed materials found to be damaged shall be replaced at contractor’s expense.

1.5	JOB CONDITIONS (CAUTIONS AND WARNINGS)

.1	Contact roofing products manufacturer for procedures when installing

a Majestic Slate – Class A Tile Roof System during temperatures less than 45ºF.

.2	Do not install the tile roof system directly over existing asphalt

shingles or existing tile roof systems.  All existing roof materials shall be removed prior to installation of new tile roof system.

.3	Roofing surface must be free of ice, water, or snow prior to and

during the roofing project.

PART 2 – PRODUCTS

2.1	GENERAL

.1	All components of the Majestic Slate – Class A Tile Roof System

are to be products manufactured or supplied by EcoStar, a Division of Carlisle SynTec Incorporated, or equal.

Note:   Only products supplied by EcoStar, a Division of Carlisle

SynTec Incorporated are included in the warranty unless otherwise specified and approved in writing.

2.2	TILES

.1	Majestic Slate – Class A Tiles made of Starloy, recycled rubber and

plastic compound, 12” wide by 18” long with a nominal thickness of ¼”.  Project shall have a 7” tile exposure (258-276 lbs. per square).  Product must have a minimum of 75% recycled materials in its composition.

.2	Majestic Slate – Class A Tile color as per the following:  10%

midnight gray, 40% Smoke Gray, 25% Earth Green, 25% Cedar Brown.  A 4’ x 8’ mockup will be supplied to the owner by the successful bidder as part of this contract to insure proper color blend selection.  Percentages may vary slightly.

2.3	RELATED MATERIALS

.1	Underlayment

.1	VersaShield – One layer of Elk VersaShield meeting or

exceeding the requirements of ASTM D226.

.2	Glacier Guard ice and water underlayment smooth surface (40

mil), a composite membrane consisting of fiberglas reinforced rubberized asphalt laminated to an impermeable polyethylene film layer.

.2	Tile Fasteners

.1	EcoStar roofing nail with a 3/8” diameter head and a minimum

of 1½”  long shank made from stainless steel.  Nails can be supplied either as a hand drive style or in coils for use in pneumatic tools.

Note:  EcoStar roofing nails must be used in the Majestic Slate – Class A Roof System and are included in the EcoStar warranty.

# PART 3 - EXECUTION

3.1  	SUBSTRATE CRITERIA

.1	The contractor is responsible for providing and determining that the

substrate is suitable to receive the Majestic Slate – Class A Tile Roof System and the authorized contractor should not proceed until all defects have been corrected.

.2	The Majestic Slate – Class A Roof System may only be applied over:

.1	Minimum ½” plywood or OSB decking

.2	Minimum 1” tongue and groove wood decking

.3	Approved metal deck systems – for specifics contact EcoStar

technical department.

.3	Minimum slope of substrate for installation of Majestic Slate – Class A

Roof System shall be a minimum of 3/12 for 6” exposure installation and a minimum of 6/12” for 7” exposure installation.  Contact the EcoStar technical department for approval of applications on lower slopes or exceptions to this requirement.

3.2	SUBSTRATE PREPARATION

.1	The contractor is responsible for ensuring that all wet or damaged

substrate has been removed in a re-roofing application.

.2	Existing roof material must be removed and a clean substrate free of

foreign material be provided prior to the installation of the Majestic Slate – Class A Tile Roof System.  Tiles may not be installed directly over any existing roof material or system.

3.3	INSTALLATION

.1	Flashing & Sheet Metal – Install sheet metal and flashing metal in all

valleys and where required on projections furnish in accordance with Section 07600 and as indicated on the drawings.

.2	Where required, install metal starter strip at all eaves and roof edges.

Furnish metal in accordance with Section 07 62 00.

.3	EcoStar suggests that all metal work be made from copper, stainless

steel or an equally long-term material.

.4	Underlayment

.1	Glacier Guard Ice and water underlayment 100% roof deck

coverage is required for this project.

.1	Lap end joints 6” and side joints 3.5”.

.2	Apply continuous 36” wide sheet in valley centered over

valley.

.3	Apply rows of 36” wide sheets along all eaves and rakes.

Lap end joints 6” and side joints 3½”.

.4	Apply rows of 36” wide sheets along and around all

dormers and roof projections.  Lap end joints 6” and side joints 3½”.

.5	Install on all had walls or vertical walls.

.6	Do not leave Glacier Guard Smooth surface exposed to

weather more than 30 days after beginning of installation.

.2	VersaShield

.1	Apply 42” wide sheet over complete deck, covering the

entire roof deck.  Lap end joints 4” and side joints 6”.

.2	Lap the VersaShield 6” from both sides over all hips,

valleys and ridges.

.3	Where the roof meets a vertical surface, carry the

VersaShield 3” to 4” up the surface.

.4	Do not leave exposed to weather more than 30 days after

beginning of installation without written approval of owner.

.5	Do not leave any fastener heads exposed.  Nail only in

areas to be covered by lapping of underlayment.

.5	Majestic Slate – Class A Tile Installation

.1	After installing underlayment and before installing the Majestic

Slate – Class A Tiles, clean the surface of debris and dirt.

.2	Beginning at the eave, install a layer of Majestic Slate – Class A

tiles gapped a minimum of 3/8” between tiles and any projections, with two roofing fasteners per tile (in location shown on tiles).  This layer of tiles will become the starter row.  Install another layer of tiles in the same manner as the first with the exception of the second layer having a ½ tile offset to the first layer.

.3	Continue installing tiles per the chosen exposure.  As tiles are

installed up the roof slope, it is recommended that lines be snapped both horizontally and vertically, using white chalk only.

.4	Care must be taken to place tiles so color variations are evenly

distributed over the entire roof area.  Tiles between bundler and pallets must be shuffled to insure even distribution of color variations.  “Patchy” or “blotchy” in appearance is not acceptable and the contractor will be required to correct.  It is recommended that work not begin until all materials have been delivered to the job site.

.5	It is the responsibility of the contractor to insure that all tiles are

bent back in a downward curve prior to installation.  Do not install tiles with an upward curve.

.6	The use of any asphaltic-based flashing cements or

caulks is strictly prohibited.  It is recommended that a one-part urethane caulk such as NP-1 be used.

.7	Either an open or closed valley design may be used.

.1	With an open valley design, leave a minimum of 2” on

each side of the center of the valley exposed and uncovered by the roof tiles.  A V-Style or W-Style valley metal may be used.

.2	With a closed valley design, cut the tiles in a straight line

to fit no closer than 3/8” against tile of adjoining roof slope.

.8	Minimum Fastening – No less than 2 fasteners per tile shall be

used with a minimum length of 1½”.

.9	Caution:  When using a pneumatic nailer, care should be taken

to insure that nails are not over driven causing the tiles to curl upward.  If tiles have been installed with over driven nails, causing the ends of the tile to curve upward, tiles will never lay flat.  Overdriven tiles must be removed and re-nailed properly.

.10	Install EcoStar Attic Guard ridge vent system per the

manufacturer’s application instructions, and then place the tiles over the ridge vent.  A minimum 2” stainless steel, hand-driven fastener  should be used to fasten the hip/ridge tile to the deck. Place fasteners in the location marked on the tile.  Tile must be installed with 6” exposure.

.11	Majestic Slate – Class A Tiles may not be installed if the tiles

have been stored in temperatures lower than 45ºF.  If tiles have been stored in temperatures below 45ºF, tiles must be brought back to an ambient material temperature of 45ºF.  As the temperature rises, tiles will expand beyond the designed installation pattern if the product is installed while cold or frozen.

.12	Do not install tiles directly adjacent to each other.  A minimum

gap of 3/8” must be maintained between installed tiles.

.13	After the initial row of tiles has been installed, it is

recommended that a chalk line be placed parallel to the roof edge and running perpendicular to the first row of tiles.  This chalk line will insure that the tiles stay true and plumb to the roof edge throughout installation.

.14	Care must be taken to minimize foot traffic over completed

areas of the roof.  Tiles will show mud and dirt and cause appearance problems.  The removal of dirt and debris is the responsibility of the contractor.

.15	Tiles can be slippery when wet.  Caution should be exhibited

with early morning dew and after rain.  EcoStar suggests the use of toe boards and OSHA approved harnesses and safety equipment at all times.

.16	Upon completion of the roof system installation, inspect and

remove all debris from roof.  Sweep clean and wash with a mild, non-bleaching detergent.

END OF SECTION