# PART 1 - GENERAL

1.01 	RELATED DOCUMENTS

1.   	Drawings and general provisions of Contract, including General Conditions and Division 1 General Requirements sections, apply to work of this section.

1.02 	DESCRIPTION OF WORK

1.   	Provide tile work including:

.1	Ceramic Mosaic Tile replacement.

.2	Regrouting of the pool.

1.03 	QUALITY ASSURANCE

1.   	Tile Manufacturing Standard: ANSI A137.1 - 1988.  Furnish tile complying with Standard Grade requirements unless indicated otherwise.

2.   	Handle, store, mix and apply proprietary setting and grouting materials in compliance with manufacturer's instructions.

3.   	Provide materials obtained from one source for each type and color of tile, grout, and setting materials.

4.   	Acceptable manufacturers shall be Dal-Tile Corp., American Olean,  U.S. Ceramic, or Buchtal.

1.04 	SUBMITTALS

1.   	Submit manufacturer's technical information and installation instructions for materials required, except bulk materials.  Include certifications and other data to show compliance 	with these specifications.

2.   	Include samples of grout and accessories requiring color selection.

1.05 	PRODUCT HANDLING

1.   	Deliver packaged materials and store in original containers with seals unbroken and 	labels intact until time of use, in accordance with manufacturer's instructions.

1.06 	JOB CONDITIONS

1.   	Maintain environmental conditions and protect work during and after installation in accordance with referenced standards and manufacturer's printed recommendations.

# PART 2 - PRODUCTS

2.01 	TILE PRODUCTS

1.   	Floors: Ceramic Mosaic Tile; Natural clay type 1"x 1", for patching areas in the pool. Color to match existing tile.

2.   	Trim and Special Shapes:  Select trim and shapes to match existing profiles where tile is damaged or removed to complete work.

2.02 	MORTAR AND GROUT

1.   	Pool Grout: White Portland cement with silica sand (2 parts sand, 1 part Portland cement).

2.   	Latex Portland cement Mortar.

3. 	Tile and grout cleaner: Sure Klean “ Standoff” grout and tile cleaner or product specifically acceptable to manufacturer of tile and grout.

4.	Degreaser: Sure Klean “EnvironKlean” degreaser.

5. 	Mortar and grout remover: Sure Klean “EnvironKlean” mortar and grout remover or product specifically acceptable to manufacturer of tile and grout.

# PART 3 - EXECUTION

3.0l 	TILE INSTALLATION STANDARDS

1.   	Comply with applicable requirements of the following, except as otherwise indicated.

.1	ANSI Al08.5:  Floor tile installed with dry-set Portland cement mortar or latex-	Portland cement mortar.

.2	All installations shall comply with TCA recommendations for materials and installation.

3.02 	INSTALLATION

- Drain swimming pool (by RCSD)

2.	After pool is drained, provide a debris screen over drain to prevent grout debris from getting into piping.

3.	Provide misting sprinklers within plunge area to keep plunge tile continuously wet/damp. Do not allow tile to become dry.

4.	Clean pool plunge area with a degreaser to remove any oil and grease films.

5.	Scrub pool plunge area with grout and tile cleaner to remove grout stains, sealers etc.

6.	Reattach/replace all loose tile within plunge area. Where existing tile is missing, provide new tile in shape and size as required for a clean, neat, smooth appearance and feel. (for bidding purposes, assume 2% of total tile area - approximately 45 sf.)

7.	Power wash pool plunge to remove all loose existing grout. Do not skim coat existing grout.

8.	Regrout pool plunge. Trowel on, sponge off.

9.	Clean residual grout scum off tiles.

10.	Snake pool drain out prior to refilling the pool.

11.	Fill pool (by RCSD) within 1-2 days of t he tile work being completed and inspected by architect.

3.03 	CLEANING AND PROTECTION

1.   	Upon  completion of placement and grouting, clean all ceramic tile surfaces so they are free of foreign matter.

2.   	Leave finished installation clean and free of cracked, chipped, broken, unbonded, or otherwise defective tile work.

END OF SECTION